## Slide 1: Functional steel/ceramic layer systems as interconnects for electrochemical energy conversion devices.
Supervisors:
prof. dr hab. inż. Tomasz Brylewski
prof. dr hab. Mieczysław Jurczyk
12.05.2023, Kraków
Kamil Domaradzki
AGH, WIMiC

## Slide 2
Motivation
Why hydrogen technologies are important?
Hydrogen can be used as a fuel
Global energy demand continues to grow
The growing importance of renewable energy sources
Moving away from environmentally harmful fossil fuels

## Slide 3
Solid Oxide Fuel Cell (SOFC)

## Slide 4
Coatings for interconnects
Problem with metallic interconnects:
Evaporation of volatile chromium compounds
Formation of poorly conductive Cr2O3 scale
Advantages of metallic interconnects:
Similar coefficient of thermal expansion with other components of the fuel cell
Easy forming process

## Slide 5
Electrophoretic deposition
Parameters of EDP
Suspesion
deposition
type of solvent
amount of dispersant (I2)
amount of powder
powder grain size
current
voltage
time

## Slide 6
Electroforetic deposition
parameters tested
12 types of solvent
Acetone
2-propanol
Ethanol
Acetone + 2-prpanol
(1:3; 1:1; 3:1)
Acetone + Ethanol
(1:3; 1:1; 3:1)
Ethanol + 2-prpanol
(1:3; 1:1; 3:1)
8 concentrations of I2
0.5 g/L
1.0 g/L
1.5 g/L
2.0 g/L
2.5 g/L
3.0 g/L
3.5 g/L
4.0 g/L
3 voltages
4 times
20 V
40 V
60 V
60 s
120 s
180 s
240 s

## Slide 7
Electroforetic deposition
EOH
IPA
ACT
ACT+EOH
ACT+IPA
EOH+IPA
25/75
50/50
75/25













## Slide 8
Electroforetic deposition

## Slide 9
Coatings after heat treatment
80 μm
69 μm
20 μm
32.5 μm
As deposited
Heat treatment
1000 °C for 5 h

## Slide 10
Composite CM/LNF
composition of the composite:
powder CM + powder LNF
wt% of LNF in composite | Sample name
5 | CM5LNF
10 | CM10LNF
15 | CM15LNF
20 | CM20LNF
30 | CM30LNF
40 | CM40LNF
50 | CM50LNF

## Slide 11
Composite CM/LNF

## Slide 12
Electrical properties

## Slide 13
Summary
To obtain nice coatings by electrophoretic deposition, it is necessary to select the appropriate deposition parameters: supspesion, dispersant concentration, voltage, current and time.
The coatings with a smooth, uniform surface were obtained from solutions containing the majority of acetone.
Analyzing the electrical conductivity and porosity of composites, the most promising coating materials are compositions with 5 and 10 wt% of LNF.

## Slide 14
Thank you!