## Slide 1: Inhalable polymeric drug delivery system: Azithromycin-loaded poly(ethylene-glycol)/poly(sebacic anhydride) microparticles
Konrad Kwiecień
AGH University of Science and Technology, Al. A. Mickiewicza 30 30-059 Kraków, Poland
kkwiecien@agh.edu.pl

## Slide 2: Motivation: Chronic Obstructive Pulmonary Disease (COPD)
Progressive life­threatening lung disease
251 million cases of COPD globally in 2016.
3.23 million deaths in 2019 (60,000 more than in 2015)
Moderate or severe lung obstruction –acute exacerbations 1.5-2 times a year, mostly due to recurrent bacterial inflammations (ca. 50% of such events)
Most of the events require hospitalization
https://www.who.int/news-room/fact-sheets/detail/chronic-obstructive-pulmonary-disease-(copd)

## Slide 3: Motivation II: Conventional therapy is not enough
Only a small portion of drugs administered orally or intravenously delivered to alveolar region of the lungs
Remaining antibiotics spread around the whole body causing severe side effects
Small concentration of antibiotic in infected area gaining resistance to antibiotics
number of potent antibiotics dimishing with each subsequent infection.
https://toxtutor.nlm.nih.gov/10-003.html
https://www.medlife.com/blog/infectious-diseases-antibiotic-resistance-growing-global-threat/

## Slide 4: Our idea
Smaller doses
Reduced side effects of systemic administration
Controlled drug release
Reduced risk of developing antibiotic resistance
Convenient form of administration
”Inhalable polymeric delivery systems of antibiotics and quorum sensing inhibitors for the treatment of respiratory infections”

## Slide 5: Project stages
I
Selection of materials with appropriate degradation kinetics and physicochemical characteristics
II
Obtaining microparticles with appropriate size distribution and encapsulation of antibiotics and QS inhibitors, testing their properties (DLS, SEM) and degradation, aerodynamic properties
III
In vitro cytocompatibility study of microparticles with pulmonary epithelial cells (A549, BEAS / 2B, and Calu-3) and ex vivo - tissue slices
IV
Determining the effectiveness of the antibacterial action
V
In vitro cytocompatibility and efficacy studies on 2.5 / 3D cell models

## Slide 6: The chosen material
Quick degradation rate
No excessive accumulation in lungs
Mostly Surface degradation
Better drug release kientics
Various copolymers
Open way for manipulating the properties
Poly(sebacic anhydride) (PSA)
PSA modified with poly(ethylene glycol) Mw = 250 or 600 10% w/w

## Slide 7: Powder manufacturing
W: poly(vinyl alcohol) (PVA) solution in UHQ-water
O: Polymer in dichloromethane (DCM)
HPLC - drug encapsulation
Microscopic observation – morphology
Zeta potential, DLS

## Slide 8: Microparticles requirements
Size: 1-5 µm
Homogeneous size distribution
Sufficient drug encapsulation capacity
Non-toxic
Bacteria eradiction in cytocompatible concentration

## Slide 9: Optical microscopy – seems perfect
Average diameter ± SD

## Slide 10: Laser diffraction size distribution, however
Peak 1 – similar to initial observation – correct sizes
Peak 2 – undetected before – incorrect sizes
Air humidity
Initial degradation
Stuck together

## Slide 11: But with PEG…
PSA-PEG 250

## Slide 12: Or with a heavier PEG
PSA-PEG 600

## Slide 13: Homogenious powders loaded with AZM
PSA-PEG250
AZM 10%
PSA-PEG600
AZM 10%
PSA-PEG250
AZM 20%
PSA-PEG600
AZM 20%
PSA-PEG250
AZM 30%
PSA-PEG600
AZM 30%

## Slide 14: And some size numbers
Batch/ feature ± SD | PSA-PEG250 AZM10% | PSA-PEG250 AZM20% | PSA-PEG250 AZM30% | PSA-PEG600 AZM10% | PSA-PEG600 AZM20% | PSA-PEG600 AZM30%
X < 5 µm | 63.05 +/- 0.87 % | 67.28 +/- 0.70 % | 76.65 +/- 0.72 % | 89.88 +/- 0.01 % | 82.82 +/- 2.76 % | 83.24 +/- 0.70 %
x50 | 3.47 +/- 0.06 µm | 3.24 +/- 0.04 µm | 2.84 +/- 0.03 µm | 2.02 +/- 0.00 µm | 2.58 +/- 0.07 µm | 2.57 +/- 0.03 µm
Span | 5.61 +/- 0.11 µm | 4.22 +/- 0.05 µm | 2.97 +/- 0.15 µm | 2.11 +/- 0.01 µm | 2.33 +/- 0.39 µm | 2.17 +/- 0.04 µm

## Slide 15: Encapsulation efficiency by HPLC – promising but not convincing
Retention time of AZM = 5.5 min
Drug: | AZM
EE | ~100%
DL | Up to 17%

## Slide 16
Flowability – fair to good, which is good!

## Slide 17
Cytotoxicity in vitro AlamarBlue

## Slide 18
Cytotoxicity in vitro Live/dead staining

## Slide 19
Cytotoxicity ex vivo rat lung tissue slices
https://www.sciencedirect.com/science/article/pii/S0939641118308993
ATP/protein test
Medium LDH
Medium ELISA IL-6
H-E staining (pending)

## Slide 20
Cytotoxicity ex vivo rat lung tissue slices

## Slide 21
Cytotoxicity ex vivo rat lung tissue slices
 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
A | 0,083 | 0,084 | 0,074 | 0,07 | 0,066 | 0,075 | 0,069 | 0,074 | 3,5 | 3,5 |  | 
B | 0,07 | 0,068 | 0,066 | 0,058 | 0,061 | 0,082 | 0,081 | 0,079 | 2,36 | 2,161 |  | 
C | 0,068 | 0,066 | 0,066 | 0,055 | 0,07 | 0,057 | 0,06 | 0,067 | 1,116 | 1,15 |  | 
D | 0,064 | 0,063 | 0,056 | 0,052 | 0,082 | 0,069 | 2,594 | 0,063 | 0,553 | 0,544 |  | 
E | 0,064 | 0,071 | 0,053 | 0,056 | 0,077 | 0,058 | 0,051 | 0,053 | 0,217 | 0,253 |  | 
F | 0,074 | 0,064 | 0,07 | 0,062 | 0,065 | 0,065 | 0,05 | 0,058 | 0,117 | 0,165 |  | 
G | 0,069 | 0,066 | 0,067 | 0,06 | 0,07 | 0,065 |  |  | 0,101 | 0,134 |  | 
H | 0,055 | 0,079 | 0,081 | 0,073 | 0,064 | 0,07 |  |  | 0,065 | 0,074 |  | 
IL-6

## Slide 22
Antibacterial properties – Kirby-Bauer test with Staphylococcus aureus

## Slide 23
Antibacterial properties – Kirby-Bauer test with Staphylococcus aureus

## Slide 24
• Successful microparticles manufacturing efficiently loaded with azithromycin
• Inhibition of S. aureus at the cytocompatible concentrations
• Hypothetically possible encapsulation of more azithromycin
• Suitable size distributions by 3 bar dispersion. What if lower?
• Bigger than under the microscope? Agglomeration…
• Future studies: the use of inhaler and lower pressures with other steps to increase the flowability and decrease agglomeration:
o Addition extra amount of free PEG as Surface modification
o Using porosity generating agents
In general, the solution is promising and PSAEG600 seems to be a better materials for this purpose than PSAEG250, but more has to be done in terms of aerodynamic properties in the next steps
Conclusions

## Slide 25: Thank you for your attention!