## Slide 1: Feasibility study and validation of PEEK gasket for DONES STUMM module
February 2005
Urszula Wiącek1, Santiago Becerril2, Jesus Castellanos3, Jerzy Kotuła1, Wojciech Królas1, Arkadiusz Kurowski1, Agnieszka Kulińska1, Jacek Świerblewski1
1 Institute of Nuclear Physics Polish Academy of Sciences (IFJ PAN), Kraków, Poland 2 IFMIF-DONES España, Granada, Spain 3 Universidad Castilla La Mancha (UCLM), Toledo, Spain
This work has been carried out within the framework of the EUROfusion Consortium, funded by the European Union via the Euratom Research and Training Programme (Grant Agreement No 101052200 — EUROfusion). Views and opinions expressed are however those of the author(s) only and do not necessarily reflect those of the European Union or the European Commission. Neither the European Union nor the European Commission can be held responsible for them.

## Slide 2
Department of Radiation Transport Physics (NZ61)
Jan Dankowski
Barbara Gabańska
Andrzej Igielski
Wojciech Królas
Agnieszka Kulińska
Arkadiusz Kurowski
Urszula Wiącek
Division of Scientific Equipment and Infrastructure Construction (DAI)
Dariusz Bocian
Marcin Curyło
Jerzy Kotuła
Rafał Ortwein
Przemysław Wąchal
Jacek Świerblewski
Wojciech Marek
IFMIF-DONES - International Fusion Materials Irradiation Facility DEMO Oriented Neutron Source
EUROfusion Consortium WPENS Project (Work Package Early Neutron Source)
IFMIF-DONES Laboratory

## Slide 3
IFMIF-DONES Laboratory
IFMIF-DONES - International Fusion Materials Irradiation Facility DEMO Oriented Neutron Source
EUROfusion Consortium WPENS Project (Work Package Early Neutron Source)
Escúzar site (ca. 10 ha), 18 km southwest from Granada, Spain

## Slide 4
IFMIF-DONES Laboratory
IFMIF-DONES - International Fusion Materials Irradiation Facility DEMO Oriented Neutron Source
EUROfusion Consortium WPENS Project (Work Package Early Neutron Source)
Escúzar site (ca. 10 ha), 18 km southwest from Granada, Spain

## Slide 5
Test Cell (TC) - the space dedicated to irradiations.
F. Arbeiter et al., Nuclear Materials and Energy (2016)
HFTM – High Flux Test Module
STUMM –
Start Up Monitoring Module
IFMIF-DONES Laboratory
A. Ibarra et al., Nuclear Fusion 58, 105002 (2018)
W. Królas et al., Nuclear Fusion 61, 125002 (2021)

## Slide 6
STUMM – Start Up Monitoring Module
Detection systems for STUMM:
Rabbit system (RS) (x8) (1 per rig) – thermal, epithermal and fast neutrons
MFC (U238) & IC (max 140) - fast neutrons
MFC (U235) or SPND detectors (max 40) – thermal and epithermal neutrons
Gamma thermometers (max 40) – nuclear heating
Thermocouples ( max 40) – temperature
Reaction | Threshold [MeV]
In-115 (n,n’) In-115m | 0.4
Ni-58 (n,p) Co-58 | 1.0
Ti-47 (n,p) Sc-47 | 1.5
Ti-46 (n,p) Sc-46 | 3.5
Ti-48 (n,p) Sc-48 | 7.0
Nb-93 (n,2n) Nb-92m | 8.9
Ni-58 (n,2n) Ni-57 | 12.4
Cu-63 (n,3n) Cu-61 | 20.0
Y-89 (n,3n) Y-87m | 21.5
Bi-209 (n,4n) Bi-206 | 22.6
Tm-169 (n,4n) Tm-166 | 23.7
Container
Single Rig
Rabbit System
Active part of rig

## Slide 7
STUMM – Start Up Monitoring Module
STUMM Ver. 2022
Rigs
Rabbit system
Electrical conectors
Initial Conditions | 
Gas pressure in Test Cell | 0.2 bar
Gas pressure in STUMM (Helium gas) | 3 – 3.5 bar
Maximum drop pressure in STUMM | 0.6 – 0.8 kPa
The maximum mass flow rate of the cooling medium | 0.18 kg/s
Cooling gas temperature at the inlet | max to 60C
Maximum temperature of the cooling gas at the outlet | 150C
Maximum temperature inside Container | 200C - 250C
Heat generation | from MCNP calculations
Neutron flux density | up to 1014 - 1015 n/cm2/s
Gamma-ray dose | ~GGy per year
Heat exchange (radiation, conduction in He-gas) with the Target Assembly at 300 C | 
The tolerated leakage for each flange shall be equal to 2  10-4 Pa  m3/s based on a total tolerated leakage from HFTM to TC of 10-2 Pa  m3/s | 

## Slide 8
It is very difficult to ensure both
Requirements:
STUMM shall be able work in more than one irradiation cycle - replaceable rigs
STUMM shall be a system tightness
STUMM Ver. 2022
General issues:
Each rig must be sealed.
Large amount of detectors in the current design (240).
2 or 3 multi-pin (20 pins) connectors per rig for the most instrumented rigs.
Limited space for access via RH.
STUMM – Start Up Monitoring Module
Rigs
Rabbit system
Electrical conectors

## Slide 9
PEEK as a gasket for STUMM
The general assumptions:
Propose material for the rigs gasket –
PEEK (Polyether ether ketone)
  One gasket for all rigs
STUMM Ver. 2022
Rigs
Rabbit system
Electrical conectors

## Slide 10
There is a risk that the PEEK seal will lose its properties and will not be reusable.
At the upper part of HFTM/STUMM is foreseen above 50 MGy / fpy.
Radiation resistance of PEEK:
Based on ITER Report (RHYTUK): Radiation damage properties of Polyether ether ketone (PEEK)
Good radiation resistance and keep its mechanical properties up to 10 – 20 MGy
Is recommended to use for the radiation dose up to 1.5 MGy
Most of the presented tests for gamma ray (or electron beam)
For combined radiation fields (neutrons and gamma) PEEK degrades faster
The parameters of PEEK are improved while the dose is increased
PEEK as a gasket for STUMM
MGy/fpy
The absorbed dose (MGy/fpy) of PEEK (Rep EFDA 2NF525 v.1.4).

## Slide 11
Experimental validation of the PEEK gasket reusing
A simple system consisting of following elements:
The vacuum chamber
PEEK o-ring seals
He leak detector
A set of pipes
The vacuum pumping station
The general questions are:
Is this solution feasible?
Is it possible to reuse the same gasket (PEEK) after rig replacemant?
PEEK as a gasket for STUMM

## Slide 12
Results of the tightness test of the seal made of PEEK
  Revision of the design & requiremants
Positive
Negative
  Other materials for rig gasket
Positive
OK!
  Radiation hardness test
Negative
Experimental validation of the PEEK gasket reusing
  Mechanical test

## Slide 13
Set-up for test experiments:
High vacuum chamber (Pressure during typical experiments up to ~3x10-6 mbar)
The front flange DN 210 ISO-K (uses clamp fasteners)
The rear flange DN 210 ISO-F (uses bolt fasteners).
Pumping system – the set of the rotary and turbo pump
Pressure measurement - IONIVAC gauge (Cold Cathode/Pirani Combination Gauge) can measure ~10-10 mbar
Pressure control - COMBIVAC gauge controller
PEEK gaskets
High vacuum chamber
Pressure control
Pressure measurement
Pumping system
Air Valves
DN 210 ISO-K
DN 210 ISO-F
Experimental validation of the PEEK gasket reusing

## Slide 14
PEEK gaskets
PEEK gasket dimensions:
A (mm) B (mm) C (mm) D (mm)
I 210 223 3 6.5
II 210 223 4 6.5
III 210 238 3 14
IV 210 238 4 14
Experimental validation of the PEEK gasket reusing
High vacuum chamber
Pressure control
Pressure measurement
Pumping system
Air Valves
DN 210 ISO-K
DN 210 ISO-F

## Slide 15
Experimental validation of the PEEK gasket reusing
Set-up for test experiments
Pumping system
Pressure control (GRAPHIX)
High vaccum chamber
Main experimental steps:
PEEK gasket placed under the front flanche of the HV chamber.
Closing and evacuating the HV chamber (~10-4 mbar).
Pressure control continously ~24 hours.
Opening of the chamber, visual check of the PEEK gasket, thickness control.
PEEK gasket placed again under the front flanche.
Steps repeated five times.
PEEK gasket dimensions:
A (mm) B (mm) C (mm) D (mm)
I 210 223 3 6.5
II 210 223 4 6.5
III 210 238 3 14
IV 210 238 4 14

## Slide 16
Preliminary experimental results
Experimental validation of the PEEK gasket reusing

## Slide 17
Results of the tightness test of the seal made of PEEK
  Revision of the design & requiremants
Positive
Negative
  Other materials for rig gasket
Positive
OK!
  Radiation hardness test
Negative
Experimental validation of the PEEK gasket reusing
  Mechanical test

## Slide 18
The first results look promising!
The next step will be a test of the PEEK gasket after irradiation
But the question is:
  Where this gasket can be irriadiated?
- MARIA Reactor
- TR24 at NPI-Rez in Czech Republic
- LIPAc
Summary

## Slide 19
References:
U. Wiącek, A. Kurowski, J. Kotuła, R. Ortwein. System Design Description Document for the IFMIF-DONES Start-Up Monitoring Module (STUMM); Technical Report - EFDA_D_2MNBDB (2023)
U. Wiącek, J. Kotuła, A. Kurowski, R. Ortwein “2022 Update of the STUMM Engineering Design”; Report EFDA_D_2PWFB8 (2023)
3D CAD model of STUMM; EFDA_D_2N5PTM v.2.9 (2023)
R. Ortwein, U. Wiącek; Conjugated heat transfer analysis of the Start-Up Monitoring Module (STUMM) for IFMIM-DONES including heat generation mapping ; Fusion Eng. Des. 188 (2023) 113451; DOI: https://doi.org/10.1016/j.fusengdes.2023.113451
C. Torregrosa-Martin and all, Overview of IFMIF-DONES diagnostics: Requirements and techniques; Fusion Eng. Des 191 (2023) 113556
U. Wiącek, and all, New approach to the conceptual design of STUMM: a module dedicated to the monitoring of neutron and gamma radiation fields generated in IFMIF-DONES, Fusion Eng. and Design 172, 112866 (2021).
W. Królas, A. Ibarra and all, The IFMIF-DONES fusion oriented neutron source: evolution of the design, Nucl. Fusion 61, 125002 (2021).
R. Ortwein, J. Kotuła, U. Wiącek, J. Świerblewski, D. Bocian, Hydraulic analysis of the start-up monitoring module (STUMM) for IFMIF-DONES, Fusion Eng. Des., 171 (2021) 112601, doi: 10.1016/j.fusengdes.2021.112601,

## Slide 20
Thank you for your attention

## Slide 21: IFMIF-DONES principal system
Accelerator Vault
Lithium Systems
Access Cell
RF area
TIR
Complementary experiments area
Test Cell (Target + Test Systems)
70% Availability
30 years Operation
System engineering approach
Poster D. Sánchez-Herranz, TUPM019
A. Ibarra et al., Nuclear Fusion 58, 105002 (2018)
W. Królas et al., Nuclear Fusion 61, 125002 (2021)

## Slide 22: DONES Programme Schedule
+1-2 years of irradiation and +1-2 years of PIE
First materials data around T0+(13-15)y
Some acceleration could be possible, but not very relevant