## Slide 1: Exploring the electronic structure of Zinc Selenide Quantum Dots
dr Rafał Fanselow
Supervisor: dr hab. Jakub Szlachetko (prof. UJ)
Assistant supervisor: dr hab. inż. Joanna Czapla-Masztafiak
Department of Applied Spectroscopy (NZ53)
Kraków, 19.12.2024

## Slide 2
What are quantum dots?
Bulk semiconductors:
continuous conduction and valence bands;
charge carriers (conduction band electrons and valance band holes) move freely within the material.
Quantum dots (QDs):
nanometer size (typically 2-10 nm);
charge carriers spatially confined;
discreate (atom-like) energy structure;
size-dependent tunable properties!
Band-like structure of bulk semiconductors and discrete energy levels of QDs

## Slide 3
García de Arquer et al., Science 373, 640 (2021)
But:
Most QDs contain toxic heavy metal elements, primarily cadmium (Cd) and lead (Pb);
new directives/laws limit the use of Cd- and Pb- in commercial technologies;
there is an ongoing search for alternatives, currently much less explored.
QDs technologies
2023 Nobel Prize in Chemistry to L. Brus, M. Bawendi, A. Ekimov and "for the discovery and synthesis of quantum dots„.
Quantum dots have potential applications in numerous fields of industry.
3
Motivation

## Slide 4
Zinc selenide quantum dots:
Aim: Characterize the effects influencing the electronic structure of ZnSe QDs.
4
Aim
Wide bandgap of bulk semiconductor (2.65 eV);
analogous structure to Cd-based QDs, thus similar synthesis schemes, precursors, etc.;
more reactive, prone to undergo reactions affecting QDs properties.

## Slide 5
5
Conducted experiments
2. X-ray spectroscopy studies
1. Material preparation & characterization
3. Time-resolved studies of carrier dynamics
Laboratory-based spectroscopy at IFJ PAN
Synchrotron measurements at SOLARIS
Steady-state optical spectroscopy
Determination of particle sizes
Optical transient absorption spectroscopy
X-ray Chronoscopy
X-rays & X-ray spectroscopy
UV/Vis photons &
Optical spectroscopy
inner-shell transitions
bulk sensitivity
element specific
chemical/structural sensitivity
band gap size
outer-shell electron transitions

## Slide 6
1. QDs preparation
Heat up wet chemical synthesis
STEM image
6
Material characterization
Scanning transmission electron microscopy (TEM)
Steady-state UV-VIS absorption & emission spectroscopy
temperature-separated stages
protective capping agents
N2 atmosphere
size control

## Slide 7
2a. Laboratory X-ray spectroscopy at IFJ PAN
7
[1] R. Fanselow, M. Sobstel, W. Błachucki, J. Szlachetko, „Performance of a laboratory von Hámos type x-ray spectrometer in x-ray absorption spectroscopy study on 3d group metals”, X-ray Spectrometry 52 (2023) 247-253. https://doi.org/10.1002/xrs.3317
low concentration
agglomeration & sedimentation
Challenges with nanomaterial suspension analysis:
Laboratory-based von Hámos type X-ray spectrometer
Simultaneous X-ray absorption spectroscopy (XAS) and X-ray emission spectroscopy (XES);
ambient conditions, easy sample manipulation;
routine sample examination.

## Slide 8
8
[2] R. Fanselow, A. Wach, W. Błachucki, J. Szlachetko, „Microliter-stirred sample setup for X-ray spectroscopy analysis of nanomaterials in suspension”, Spectrochim. Acta Part B At. Spectrosc. 189 (2022) 106367. https://doi.org/10.1016/j.sab.2022.106367
2a. Sample cell for laboratory X-ray spectroscopy
Commonly available & inexpensive components
Sample volumes down to 50 µL
Continuous sample mixing during the measurement

## Slide 9
2a. Laboratory X-ray spectroscopy
Laboratory Zn K-edge XAS:
qualitative assessment of observable spectral changes;
intensity increase of 1s→4p transition has been attributed to presence of Zn vacancies in other Zn nanostructures [3];
pronounced structural changes in the photoelectron scattering region.
9
[3] Rossi, T. et al. Characterizing the Structure and Defect Concentration of ZnO Nanoparticles in a Colloidal Solution. J. Phys. Chem. C 2014, 118 (33), 19422–19430. https://doi.org/10.1021/jp505559u
1s
4p
…
Continuum
XAS
Zn K-edge XAS
Absorption coefficient (a. u.)
Photon energy (eV)
Difference (a. u.)
Photon energy (eV)

## Slide 10
2b. Synchrotron studies
ASTRA beamline
Zn K-edge XAS
More intense X-ray source & improved signal quality
10
surface atom
surface atom coordinated with ligand
Se vacancy
Zn vacancy
Calculations in FEFF 9.6 using several model structures with different coordination of central Zn atom

## Slide 11
Sample
White beam
probe pulse
Delay
Time
Monochromatic pump pulse
3a. Ultrafast optical transient absorption
Pump-probe
experiment
Ultrashort monochromatic pulse (pump) triggers the reaction/process in a studied sample.
White probe pulse follows at a defined delay and captures the current state of the specimen.
The result is compared to the sample in the ground state (acquired without pump pulse).
The measurement is repeated for another pump-probe delay value.
Transient signal:
11
Temporal resolution of experiment: ~100fs
ELI Beamlines
Dolní Břežany

## Slide 12
12
Photoinduced absorption
Ground state bleach decay
Two main relaxation channels showing different dependence on quantum dot size:
τ1 ~ 0.35-0.95 ps, 64-90%
τ2 ~ 2-3 ps, 8-28%
Ground state
Excited state
Pump pulse
Photoinduced absorption states
Probe
Excitation with pump pulse
Normalized ΔA (a. u.)
Absorbance
Photon Energy (eV)
Photon Energy (eV)
TA spectra
3a. Ultrafast optical transient absorption

## Slide 13
3b. X-ray Chronoscopy
13
sample
X-ray pulse
Optical pump pulse
pump-probe experiment
time
Proposal to expand time-resolved measurements of electron dynamics in QDs with the use of X-ray free electron lasers and X-ray chronoscopy method.
Intensity (a. u.)

## Slide 14
3b. X-ray Chronoscopy
14
sample
Incident X-ray pulse
Optical pump pulse
pump-probe experiment
time
Proposal to expand time-resolved measurements of electron dynamics in QDs with the use of X-ray free electron lasers and X-ray chronoscopy method.
Intensity (a. u.)
Transmitted X-ray pulse

## Slide 15
15
Numerical simulations of X-ray pulse propagation through a sample excited by an optical pulse were performed using the time-dependent Lambert–Beer law and a four-level sample model;
the impact of X-ray pulse duration and number of pump-probe cycles on the precision of the excited state lifetime determination was investigated;
results showcased that X-ray Chronoscopy can be utilized to track electron dynamics in matter, including ZnSe QDs.
3b. X-ray Chronoscopy

## Slide 16
Conclusions
16
Within my doctoral project:
I prepared a series of ZnSe quantum dot suspensions and determined their size-dependent optical properties.
I developed a special sample cell to enable X-ray measurements of QDs liquid suspensions.
I conducted X-ray spectroscopy measurements that indicated the presence of zinc defects in the examined quantum dots.
I determined the main carrier relaxation processes using ultrafast transient optical spectroscopy.
I proposed an X-ray Chronoscopy method as a complementary method for studying carrier dynamics in quantum dots.

## Slide 17
This work was supported by the National Science Centre (Poland) under grants number 2020/37/B/ST3/00555 and 2017/27/B/ST2/01890
Special thanks to all the members of the department of the Applied Spectroscopy at IFJ PAN:
Prof. W. M. Kwiatek Dr. hab. J. Czapla-Masztafiak Dr. W. Błachucki Dr. G. Imbir Dr. A. Yakovliev T. Pieprzyca
and to my supervisor Prof. J. Szlachetko.
17