## Slide 1: Influence of irradiation on the magnetic properties of coordination polymers
2nd Workshop on Research & Innovation in Poland
IFJ PAN, Krakow, 26-27 May, 2026
Piotr Konieczny, Dominik Czernia

## Slide 2
6.66 MeV
J. Appl. Phys. (2009)
10 and 40 MeV
New J. Phys. 10 (2008)
2 MeV
Appl. Phys. Lett. (2012)
50 keV
JMMM 333(2013)
MoS2
2.25 MeV
Phys. Rev. Lett. 91 (2003)
Graphite
Li0.5Fe2.5O4
Magnetism and proton irradiation

## Slide 3
Influence of proton irradiation
on the magnetic properties of 2D Ni(II) molecular ferrimagnet

## Slide 4
NiIISO4(1,3-phenylenediamine)2
D. Czernia
Tc = 24 K
PXRD, IR, DC magnetometry
Sci Rep 13, 14032 (2023)

## Slide 5
NiIISO4(1,3-phenylenediamine)2
Sci Rep 13, 14032 (2023)
Tc = 24 K
PXRD, IR, DC magnetometry
D. Czernia
Van de Graaff accelerator
1.9 MeV protons
10 nA

## Slide 6
Sci Rep 13, 14032 (2023)
Pellet thickness
> 100 μm
Sample preparation issue

## Slide 7
Sci Rep 13, 14032 (2023)
Pellet thickness
> 100 μm
Sample preparation issue
Van de Graaff accelerator
1.9 MeV protons
10 nA
two phases!

## Slide 8
Sci Rep 13, 14032 (2023)
Powder layer thickness
≈ 30 μm

## Slide 9
Sci Rep 13, 14032 (2023)
coercive field: reduction up to 90%
maximal magnetization (at 7T): 65% -150% of the reference sample
degree of irreversibility Δχirr: increase up to 40%
Temperature of phase transition: constant
Powder layer thickness
≈ 30 μm

## Slide 10
Sci Rep 13, 14032 (2023)
coercive field: reduction up to 90%
maximal magnetization (at 7T): 65% -150% of the reference sample
degree of irreversibility Δχirr: increase up to 40%
Temperature of phase transition: constant
Reference
5 x 1013 cm-2
1014 cm-2
2.5 x 1014 cm-2
2 x 1015 cm-2
Infrared spectroscopy

## Slide 11: Which Section (1, 2 or 3) Required beam: particle, energy nad properties
Section 1 and 2 – depending on investigated material
All available particles with variable energy
Beam current range: 1 nA - 20 nA – to limit sample degradation
No requirements about time structure of the beam

## Slide 12: Other requirements (detection system, infrastructure)
Sample conditions:
scanning stage with cooling – to limit healing effect,
Energy degraded beam – uniform modification,
Real-Time Data: setup for electrical transport measurements and other techniques (magnetic, optic).

## Slide 13
GSI
Helmholtzzentrum für Schwerionenforschung
Darmstadt

## Slide 14
GSI
Helmholtzzentrum für Schwerionenforschung
Darmstadt
M1 Beamline – Scanning electron microscope and ToF-SIMS/SNMS
M2 Beamline – X-ray diffraction
M3 Beamline – In-situ spectroscopy and oven chamber

## Slide 15
Phys. Rev. Research 8, 023054
Published 16 April, 2026

## Slide 16: SWOT analysis for the project
Strengths
Builds on existing expertise in post-irradiation characterization.
Combines irradiation with real-time electrical transport and UV-VIS measurements,.
Creates a unique experimental capability in Poland and fills a clear infrastructure gap.
Weaknesses
Risk of sample degradation during irradiation, especially for sensitive materials.
Requires a highly flexible beamline: adjustable energy, current, and sample environment.
In situ experiments are technically demanding, e.g. complex integration of optical diagnostics.
Opportunities
Fits the growing concept of defect engineering in functional materials.
Strong relevance for advanced materials research, including radiation-tolerant and tunable systems.
Threats
Competing laboratories may develop similar in situ capabilities.
High investment and operating costs could constrain long-term sustainability.

## Slide 17: Conclusions
Development of an in situ ion-irradiation beamline enabling real-time electric transport and UV-VIS measurements
Direct insight into defect-driven modification of functional materials
Platform for interdisciplinary collaboration
Scalable concept with strong potential for application-oriented and industrial research

## Slide 18
thank you for your attention